Kézite K700
Lead Zirconate Titanate Piezoelectric Ceramic with High Coupling,
and Very High Dielectric Constant and Piezoelectric Constant

K700 is a modified lead zirconate titanate piezoelectric ceramic that has a high coupling, and very high dielectric constant and piezoelectric constant. The high permittivity and high piezoelectric constant make it an excellent choice for 1-3 composites, multi-element arrays, and actuator applications.

K700 PHYSICAL & ELECTRICAL PROPERTIES. KT33; Free Dielectric Constant; 4000. KS33; Clamped Dielectric Constant; 1830. k33; Longitudinal Coupling Coefficient; 0.75. k31; Transverse Coupling Coefficient; 0.42. k15; Shear Coupling Coefficient; 0.72. kt; Thickness Coupling Coefficient; 0.52. kp; Planar Coupling Coefficient; 0.71. d33; Piezoelectric Strain Constant (x 10-12 m/V); 700. d31; Piezoelectric Strain Constant (x 10-12 m/V); -290. d15; Piezoelectric Strain Constant (x 10-12 m/V); 950. g33; Piezoelectric Voltage Constant (x 10-3 Vm/N); 19.8. g31; Piezoelectric Voltage Constant (x 10-3 Vm/N); -9. g15; Piezoelectric Voltage Constant (x 10-3 Vm/N); 28. sE33; Compliance at Constant Field (x 10-12 m2/N); 19. Qm; Mechanical Q (Thickness); 30. Qm; Mechanical Q (Radial); 65. YE33; Young's Modulus at Constant Field (x 1010 N/m2); 5. D; Dissipation; 0.025. Nt; Thickness Frequency Constant (kHz-in) Thickness Frequency Constant (Hz-m); 79 2006. Np; Planar Frequency Constant (kHz-in) Planar Frequency Constant (Hz-m); 80 2032. r; Density (g/cm3); 7.7. ZA; Acoustic Impedance (MRayL); 35. Vs; Sound Velocity (m/sec); 4615. TC; Curie Temperature (ºC); 210. CTE; Coefficient of Thermal Expansion (x 10-6 in/in/ºF) (20 oC to 100 oC); 5.5. dave; Average Grain Size (mm); 3 to 5. Note: The above values are nominal...